Supplementary materials

Stability of manganese(II) phthalocyanine films in ambient air

P.A. Yunin, Y.I. Sachkov, V.V. Travkin, G.L. Pakhomov

DOI: 10.6060/mhc224426y

Supplement 1

Comparison of the experimental XRD spectrum (purified PcMn powder in Fig. 2) and the spectrum calculated using the CIF file CCDC#1212698 [18].

Supplement 2

| Top view | Isometric view |
| --- | --- |
| Views of the packing of molecules in a -PcMn film textured by the (100) plane oriented parallel to the silicon substrate (marked in gray) |  |

Supplement 3

| As-received (raw, unpurified) | Recrystallized (purified) |
| --- | --- |
| Photographs of MnPc powder in an optical microscope (200× magnification) |  |

Supplement 4

| Tg=25oC | Tg=200oC |
| --- | --- |
| Photographs of thin-film PcMn samples on various substrates used in this work after one month storage in air. |  |

Supplement 5

|  |  Redrawn from Fig. 4: Comparison of spectra of PcMn films on cold and hot substrates. |
| --- | --- |
| Spectra of the -PcMn film in air and Ar before and after one-sun illumination for 13 h (a Zolix SS150 solar simulator with AM1.5G filter) | Spectra of PcMn films with Tg=25oC on quartz (green curve) and indium-tin oxide (ITO, blue curve) |

Supplement 6

|  |  | As-deposited on Si | As-deposited on SiO2 |  |  |  |  | Tg=200oC on SiO2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tg=25oC |  |  |  |  |  | Initial |  |  |
| Tg=200oC |  |  |  |  | Stored in air for 1 month |  |  |  |
| AFM images of the surface of PcMn films deposited on silicon (left column) and quartz substrates at 25o and 200oC, before and after 1 month storage in air, cf. Fig. 6. |  |  |  |  |  |  |  |  |

Supplement 7

| WLI images of the surface of the low-temperature PcMn film after 1 month storage in air, with different magnification. Sq = root mean square roughness |  |
| --- | --- |
| Tg=200oC, stored in air | Tg=200oC, stored in Ar |
| WLI images of the surface of the high-temperature PcMn film after 1 month storage |  |

| Tg=25oC, stored in air | Tg=200oC, stored in air |
| --- | --- |
| WLI images of the bottom of crater remaining after SIMS depth profiling down to silicon substrate |  |

Supplement 8

SIMS profiles for negative secondary ions O2- and OH-, cf. Fig. 5.