Supplementary Data for

Magnetocaloric properties of lanthanide tetrapyrrole complexes above Curie temperature

Tatyana N. Lomova,a@ Victor V. Korolev,a Anna G. Ramazanova,a and Olga V. Balmasovaa

aG. A. Krestov Institute of Solution Chemistry, Ivanovo, 153045, Russian Federation

@Corresponding author E-mail: tnl@isc-ras.ru

Content

- 1H NMR specrf of (Cl)TbTP, (Cl)TbTtBuPP, and (Cl)TbPc			2-4

- IR spectra of (Cl)TbPc and (Cl)TbTtBuPP						5

- The MALDI TOF mass spectrum of samples					6,7

- The parameters of the UV-vis spectra of (Cl)TbTtBuPP in chloroform		8

- Experimental specific/molar heat capacity of samples				9-11

- The temperature dependences of samples MCE, the enthalpy change, the specific heat and the entropy change due to the samples magnetization				12-14

Figure S1. 1H NMR specrum of (Cl)TbTPP in CDCl3

Figure S2. 1H NMR spectrum of (Cl)TbtBuTP in CDCl3

Figure S3. 1H NMR spectrum of (Cl)TbPc DMF (insert  spectrum in CDCl3)

Figure S4. The IR spectra of (Cl)TbPc (top) and (Cl)TbTtBuPP (bottom)

Figure S5. The MALDI TOF mass spectrum of (5,10,15,20-Tetra(4-tert-butylphenylporphinato))terbium(III) chloride (M = 1031.5392 g mol-1). The matrix is CHCA (a), DHB (b), and without a matrix (c).

Figure S6. The MALDI TOF mass spectrum of (phthalocyaninato)terbium(III) chloride (M = 706.9104 g mol-1). The matrix is DHB

Table S1. The parameters of the UV-vis spectra of (Cl)TbTtBuPP in chloroform

| The complex | λmax, nm (logε) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Q(0,0) | Q(0,1) | Q(0,2) | B(0,0) | B(0,1)[c] |
| (Cl)ТbTtBuPP | 593 (3.97) | 555 (4.34) | 517 (3.90) | 424 (5.68) | 400 |
| (Cl)ТbTtBuPP[a] | 593 | 554 | 517 | 424 | 400 |
| (Cl)ТbTtBuPP[b] | 593 | 554 | 517 | 424 | 400 |

[a]After a DSC experiment. [b] After a microcaloric experiment (the ratio of the intensities of the absorption bands is B(0,0) > Q(0,1) > Q(0,0) > Q(0,2)). [c] A shoulder.

Table S2 Experimental specific/molar heat capacity of (5,10,15,20-tetraphenylporphinato)terbium(III) chloride (M = 807.1104 g·mol-1)

| T/К | СP/ J K-1g-1 | СP/ J K-1mol-1 | T/К | СP/ J K-1g-1 | СP/ J K-mol-1 | T/К | СP/ J K-1g-1 | СP/ J K-1mol-1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 270.07 | 1.04770 | 0.00130 | 291.07 | 1.22171 | 0.00151 | 312.07 | 1.46416 | 0.00181 |
| 271.07 | 1.05371 | 0.00131 | 292.07 | 1.23282 | 0.00153 | 313.07 | 1.47424 | 0.00183 |
| 272.07 | 1.05722 | 0.00131 | 293.07 | 1.24252 | 0.00154 | 314.07 | 1.48588 | 0.00184 |
| 273.07 | 1.06182 | 0.00132 | 294.07 | 1.25195 | 0.00155 | 315.07 | 1.49698 | 0.00185 |
| 274.07 | 1.06847 | 0.00132 | 295.07 | 1.26209 | 0.00156 | 316.07 | 1.50550 | 0.00187 |
| 275.07 | 1.07549 | 0.00133 | 296.07 | 1.27478 | 0.00158 | 317.07 | 1.51599 | 0.00188 |
| 276.07 | 1.08364 | 0.00134 | 297.07 | 1.28554 | 0.00159 | 318.07 | 1.52608 | 0.00189 |
| 277.07 | 1.09149 | 0.00135 | 298.07 | 1.29787 | 0.00161 | 319.07 | 1.53715 | 0.00190 |
| 278.07 | 1.10043 | 0.00136 | 299.07 | 1.31013 | 0.00162 | 320.07 | 1.54692 | 0.00192 |
| 279.07 | 1.10774 | 0.00137 | 300.07 | 1.32344 | 0.00164 | 321.07 | 1.55555 | 0.00193 |
| 280.07 | 1.11684 | 0.00138 | 301.07 | 1.33474 | 0.00165 | 322.07 | 1.56373 | 0.00194 |
| 281.07 | 1.12593 | 0.00140 | 302.07 | 1.34749 | 0.00167 | 323.07 | 1.57106 | 0.00195 |
| 282.07 | 1.13478 | 0.00141 | 303.07 | 1.35916 | 0.00168 | 324.07 | 1.58079 | 0.00196 |
| 283.07 | 1.14427 | 0.00142 | 304.07 | 1.37167 | 0.00170 | 325.07 | 1.58924 | 0.00197 |
| 284.07 | 1.15223 | 0.00143 | 305.07 | 1.38378 | 0.00171 | 326.07 | 1.59683 | 0.00198 |
| 285.07 | 1.16215 | 0.00144 | 306.07 | 1.39608 | 0.00173 | 327.07 | 1.60327 | 0.00199 |
| 286.07 | 1.17159 | 0.00145 | 307.07 | 1.40824 | 0.00174 | 328.07 | 1.61126 | 0.00200 |
| 287.07 | 1.18030 | 0.00146 | 308.07 | 1.42045 | 0.00176 | 329.07 | 1.61493 | 0.00200 |
| 288.07 | 1.19139 | 0.00148 | 309.07 | 1.43095 | 0.00177 | 330.07 | 1.62315 | 0.00201 |
| 289.07 | 1.20160 | 0.00149 | 310.07 | 1.44249 | 0.00179 | 331.07 | 1.62893 | 0.00202 |
| 290.07 | 1.21209 | 0.00150 | 311.07 | 1.45331 | 0.00180 | 332.07 | 1.63426 | 0.00202 |

Table S3 Experimental specific/molar heat capacity of (5,10,15,20-Tetra(4-tert-butylphenylporphinato))terbium(III) chloride (M = 1031.5392 g mol-1)

| T/К | СP/ J K-1g-1 | СP/ J K-1mol-1 | T/К | СP/ J K-1g-1 | СP/ J K-mol-1 | T/К | СP/ J K-1g-1 | СP/ J K-1mol-1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 270.07 | 1.17600 | 0.00114 | 291.07 | 1.34474 | 0.00130 | 312.07 | 1.56660 | 0.00152 |
| 271.07 | 1.18199 | 0.00115 | 292.07 | 1.35660 | 0.00132 | 313.07 | 1.57332 | 0.00153 |
| 272.07 | 1.18570 | 0.00115 | 293.07 | 1.36549 | 0.00132 | 314.07 | 1.58101 | 0.00153 |
| 273.07 | 1.19250 | 0.00116 | 294.07 | 1.37591 | 0.00133 | 315.07 | 1.59017 | 0.00154 |
| 274.07 | 1.19812 | 0.00116 | 295.07 | 1.38789 | 0.00135 | 316.07 | 1.59620 | 0.00155 |
| 275.07 | 1.20381 | 0.00117 | 296.07 | 1.39955 | 0.00136 | 317.07 | 1.60160 | 0.00155 |
| 276.07 | 1.21213 | 0.00118 | 297.07 | 1.40913 | 0.00137 | 318.07 | 1.60904 | 0.00156 |
| 277.07 | 1.21826 | 0.00118 | 298.07 | 1.42196 | 0.00138 | 319.07 | 1.61670 | 0.00157 |
| 278.07 | 1.22874 | 0.00119 | 299.07 | 1.43308 | 0.00139 | 320.07 | 1.62515 | 0.00158 |
| 279.07 | 1.23688 | 0.00120 | 300.07 | 1.44717 | 0.00140 | 321.07 | 1.62896 | 0.00158 |
| 280.07 | 1.24438 | 0.00121 | 301.07 | 1.45799 | 0.00141 | 322.07 | 1.63359 | 0.00158 |
| 281.07 | 1.25113 | 0.00121 | 302.07 | 1.47197 | 0.00143 | 323.07 | 1.63756 | 0.00159 |
| 282.07 | 1.25957 | 0.00122 | 303.07 | 1.48297 | 0.00144 | 324.07 | 1.64231 | 0.00159 |
| 283.07 | 1.26692 | 0.00123 | 304.07 | 1.49624 | 0.00145 | 325.07 | 1.64738 | 0.00160 |
| 284.07 | 1.27595 | 0.00124 | 305.07 | 1.50467 | 0.00146 | 326.07 | 1.65072 | 0.00160 |
| 285.07 | 1.28812 | 0.00125 | 306.07 | 1.51397 | 0.00147 | 327.07 | 1.65445 | 0.00160 |
| 286.07 | 1.29676 | 0.00126 | 307.07 | 1.52149 | 0.00147 | 328.07 | 1.65838 | 0.00161 |
| 287.07 | 1.30478 | 0.00126 | 308.07 | 1.53231 | 0.00149 | 329.07 | 1.65937 | 0.00161 |
| 288.07 | 1.31496 | 0.00127 | 309.07 | 1.53964 | 0.00149 | 330.07 | 1.66392 | 0.00161 |
| 289.07 | 1.32413 | 0.00128 | 310.07 | 1.54993 | 0.00150 | 331.07 | 1.66847 | 0.00162 |
| 290.07 | 1.33555 | 0.00129 | 311.07 | 1.55780 | 0.00151 | 332.07 | 1.67454 | 0.00162 |

Table S4 Experimental specific/molar heat capacity of (Phthalocyaninato)terbium(III) chloride (M = 706.9104 g mol-1

| T/К | СP/ J K-1g-1 | СP/ J K-1mol-1 | T/К | СP/ J K-1g-1 | СP/ J K-mol-1 | T/К | СP/ J K-1g-1 | СP/ J K-1mol-1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 270.07 | 0.88108 | 0.00125 | 291.07 | 0.99887 | 0.00141 | 312.07 | 1.16399 | 0.00165 |
| 271.07 | 0.88284 | 0.00125 | 292.07 | 1.00669 | 0.00142 | 313.07 | 1.17116 | 0.00166 |
| 272.07 | 0.88674 | 0.00125 | 293.07 | 1.01511 | 0.00144 | 314.07 | 1.17802 | 0.00167 |
| 273.07 | 0.89057 | 0.00126 | 294.07 | 1.02493 | 0.00145 | 315.07 | 1.18461 | 0.00168 |
| 274.07 | 0.89604 | 0.00127 | 295.07 | 1.03422 | 0.00146 | 316.07 | 1.19115 | 0.00169 |
| 275.07 | 0.90128 | 0.00127 | 296.07 | 1.04363 | 0.00148 | 317.07 | 1.19752 | 0.00169 |
| 276.07 | 0.90627 | 0.00128 | 297.07 | 1.05278 | 0.00149 | 318.07 | 1.20474 | 0.00170 |
| 277.07 | 0.91353 | 0.00129 | 298.07 | 1.06124 | 0.00150 | 319.07 | 1.21036 | 0.00171 |
| 278.07 | 0.91846 | 0.00130 | 299.07 | 1.06836 | 0.00151 | 320.07 | 1.21615 | 0.00172 |
| 279.07 | 0.92405 | 0.00131 | 300.07 | 1.07581 | 0.00152 | 321.07 | 1.22255 | 0.00173 |
| 280.07 | 0.92941 | 0.00131 | 301.07 | 1.08327 | 0.00153 | 322.07 | 1.22800 | 0.00174 |
| 281.07 | 0.93585 | 0.00132 | 302.07 | 1.09018 | 0.00154 | 323.07 | 1.23309 | 0.00174 |
| 282.07 | 0.94065 | 0.00133 | 303.07 | 1.09662 | 0.00155 | 324.07 | 1.23760 | 0.00175 |
| 283.07 | 0.94625 | 0.00134 | 304.07 | 1.10366 | 0.00156 | 325.07 | 1.24195 | 0.00176 |
| 284.07 | 0.95345 | 0.00135 | 305.07 | 1.11119 | 0.00157 | 326.07 | 1.24656 | 0.00176 |
| 285.07 | 0.95890 | 0.00136 | 306.07 | 1.11893 | 0.00158 | 327.07 | 1.25051 | 0.00177 |
| 286.07 | 0.96521 | 0.00137 | 307.07 | 1.12681 | 0.00159 | 328.07 | 1.25438 | 0.00177 |
| 287.07 | 0.97047 | 0.00137 | 308.07 | 1.13412 | 0.00160 | 329.07 | 1.25808 | 0.00178 |
| 288.07 | 0.97796 | 0.00138 | 309.07 | 1.14243 | 0.00162 | 330.07 | 1.26097 | 0.00178 |
| 289.07 | 0.98392 | 0.00139 | 310.07 | 1.15004 | 0.00163 | 331.07 | 1.26419 | 0.00179 |
| 290.07 | 0.98998 | 0.00140 | 311.07 | 1.15627 | 0.00164 | 332.07 | 1.26650 | 0.00179 |

Figure S7. The temperature dependences of (Cl)TbTPP MCE at the magnetic induction

Figure S8. The temperature dependences of (Cl)TbPc MCE at the magnetic induction

Figure S9. The temperature dependences of the enthalpy change due to the (Cl)TbTtBuPP magnetization at the magnetic induction

Figure S10. The temperature dependences of the enthalpy change due to the (Cl)TbTPP magnetization at the magnetic induction

Figure S11. The temperature dependences of enthalpy change due to the (Cl)TbPc magnetization at the magnetic induction

Figure S12. The temperature dependences of the specific heat due to the (Cl)TbTtBuPP magnetization at the magnetic induction

Figure S13. The temperature dependences of the specific heat due to the (Cl)TbTPP magnetization at the magnetic induction

Figure S14. The temperature dependences of the specific heat due to the (Cl)TbPc magnetization at the magnetic induction

Figure S15. The temperature dependences of the entropy change due to the (Cl)TbTPP magnetization at the magnetic induction

Figure S16. The temperature dependences of the entropy change due to the (Cl)TbTtBuPP magnetization at the magnetic induction

Figure S17. The temperature dependences of the entropy change due to the (Cl)TbPc magnetization at the magnetic induction