SUPPLEMENTARY MATERIALS

Influence of Substitution Patterns in A Set of BODIPY Derivatives on Aggregation Properties in Binary Solvent Mixtures.

Elena V. Antina1, Daniil D. Gryaznov2, Evgeniy E. Molchanov2,3, Valeria A. Kalinkina1,2, Alexander A. Kalyagin1, Tatiana V. Kokurina2, Lubov A. Antina1, Ksenia V. Ksenofontova2,3, Yuriy S. Marfin3 and Sergey D. Usoltsev2,3 @

1 G.A. Krestov Institute of Solution Chemistry of the Russian Academy of Sciences, Ivanovo, 153045, Russia

2 Ivanovo State University of Chemistry and Technology, Ivanovo, 153000, Russia.

3 Pacific National University, Khabarovsk, 680035, Russia

@ Corresponding author E-mail: sergeyusoltsev@yahoo.com

| (a) | (b) | (c) |
| --- | --- | --- |

Figure S1. Example electronic absorption spectra, demonstrating lack of significant changes during aggregation experiment. (a) meso-ortho-pyridine-BODIPY in water – acetonitrile mixture, (b) meso-para-pyridine-BODIPY in water – acetonitrile mixture, (c) meso-vanilin-BODIPY in water – THF mixture

| (a) | (b) |
| --- | --- |

Figure S2. Dependencies of fluorescence intensity on water content for (a) meso-ortho-pyridine-BODIPY in Water – DMSO mixtures and (b) meso-para-pyridine-BODIPY in water-DMSO mixtures. Dependencies are normalized to the first point. Black points are intensities before inflection, red points – beyond “critical” water content. λex = 530 nm, λem = 545 nm for both compounds.

| (a) | (b) |
| --- | --- |

Figure S3. Fluorescence lifetime distributions obtained from maximum entropy fitting of 100 lifetimes in Water – ACN mixtures for vanilin-BODIPY in (a) range of 0 – 8 ns up to 60 Vol.% water content and (b) range of 0 – 8 ns with water content in the range of 65 – 85 Vol.%

Figure S4. Changes in EAS maximum intensity for meso-vanilin-BODIPY in water – ACN mixture upon change in volumetric water content.