SUPPORTING INFORMATION

Novel Imidazolium Derivatives of Thiacalix[4]arenes Containing Fluorescein Fragments: Synthesis, Aggregation Properties and Photocatalytic Activity

DOI: 10.6060/mhc256787s

Elza D. Sultanova,@ Alina A. Artemenko, Ekaterina A. Bondareva, 
Ilshat M. Bogdanov, Aliya E. Akhatova, Diana A. Mironova, Vladimir A. Burilov, Svetlana E. Solovieva, and Igor S. Antipin

Kazan Federal University, 420008 Kazan, Russian Federation.

@Corresponding author E-mail: elsultanova123@gmail.com

a)

b)

C-O

Ph

CH

C-Br

c)

d)

Figure S1. NMR 1H (a), 13C (b), FT IR (c) and HRESI MS (d) spectra of (2b).

a)

b)

c)

d)

Figure S2. NMR 1H (a), 13C (b), FT IR (c) and HRESI MS (d) spectra of (4b).

a)

b)

c)

d)

Figure S3. NMR 1H (a), 13C (b), FT IR (c) and HRESI MS (d) spectra of 6a.

a)

b)

c)

d)

Figure S4. NMR 1H (a), 13C (b), FT IR (c) and HRESI MS (d) spectra of 6b.

Table 1S. Data from Boltzmann Equation.

| Model | Boltzmann |  |  |
| --- | --- | --- | --- |
| Equation | y = A2 + (A1-A2)/(1 + exp((x-x0)/dx)) |  |  |
| Reduced Chi-Sqr | 8.56E-05 | 7.38E-05 |  |
| Adj. R-Square | 0.99898 | 0.99727 |  |
|  |  | Value | Standard Error |
| D | A1 | 1.6491 | 0.00905 |
| D | A2 | 1.11111 | 0.01524 |
| D | x0 | -0.84214 | 0.03025 |
| B | A1 | 1.73661 | 0.01048 |
| B | A2 | 0.83296 | 0.00636 |
| B | x0 | -1.31381 | 0.0124 |

Figure S5. Dependence of the emission intensity of 5 (black), Flu-TCA-C4 (blue) and Flu-TCA-C8 (red) on the concentration.

Figure S6. Integrated fluorescence intensity vs max. absorbance at different concentrations for fluorescein (0.1M NaOH) and fluorescein (green), 5 (black), Flu-TCA-C4 (blue), Flu-TCA-C8 (red) (water with 50% DMF); C = 0.001-0.1 mM

Figure S8. Photo of the photoreactor.

Figure S9. Graph of the dependence of the peak area of N-phenyl-1,2,3,4-tetrahydroisoquinoline on the GC-MS spectra on its concentration.

Figure S10. NMR 1H-spectrum of the reaction mixture with a catalyst (6a), CDCl3, 25 oC.